# Print Adhesion

The shape of the object has a key role in warping. Oval shapes shrink fairly uniformly and do not tend to warp. On the other hand, rectangular shapes with sharp corners may warp. Ideally, you should design your parts to have a decently sized flat area in contact with the print surface. This will ensure good adhesion and prevent print failures due to the print detaching and being knocked off the printer.

Let’s take a look at this example object as the worst-case scenario.

worst_case.png

The tip of the model has an extremely sharp corner and minimal surface area in contact with the print surface. Furthermore, this part has minimal volume to retain heat. As a result, the tip of the model started lifting from the bed and warping upwards. As the print starts lifting/warping, the layer being printed on top of that area starts to compress, resulting in not only an undesirable look but also incorrect dimensions.

worst_case_lifting.png

If you need a similar shape as part of your design, there are two ways you can counteract warping:

- Use a brim in the slicer

- Add corner pads while designing your part

A brim consists of several additional loops around the outer edge of the part. When a brim in enabled in the slicer, the program automatically adds approximately 3mm of extra plastic all the way around the first layer of your part. This increases the surface area of the first layer to give the part more area to grip to the bed and if the plastic does begin to warp up, it is the brim that warps and not the actual part.

box_with_brim.png

Corner pads are essentially brims that are intentionally added to the model while designing the part to increase the contact area with the print surface only at sharp corners or fine areas rather than around the entire part. This makes it easier to remove the extra material during post-processing.

| corner_pad_model.jpg | corner_pad.png |
| --- | --- |